# Sub-micrometer holotomography of multiphase metals

REQUENA G.1, CLOETENS P.2, ALTENDORFER W.1, POLETTI C.1, TOLNAI D.1,3, WARCHOMICKA F1., DEGISCHER H.P.1

1Institute of Materials Science and Technology, Vienna University of Technology, Karlsplatz 13/308, Vienna, Austria (grequena@mail.zserv.tuwien.ac.at); 2European Synchrotron Radiation Facility, 6 Rue Jules Horowitz, 38000 Grenoble Cédex, France; 3Eötvös Loránd University, Department of Materials Physics, POB 32, 1518 Budapest, Hungary

Synchrotron microtomography has shown to be a powerful technique to reveal the internal architecture of materials. Furthermore, the coherence of the beam can be exploited applying quantitative phase contrast tomography or holotomography [1] to image components with similar attenuation. The spatial resolution achievable by parallel beam synchrotron microtomography is about 1 µm. This can be improved using magnifying optics. We present results obtained by magnified synchrotron holotomography using a Kirkpatrick-Baez (KB) optics system [2]. The experiments were carried out at the nano-imaging end-station ID22NI for Al- and Ti-based materials using samples with 0.4mm diameter. The focal point with a size of 80 nm (H) by 130 nm (V) and medium monochromaticity (E/E = 2x10-2) is produced by a set of multilayer coated crossed bent mirrors. Energies of 17.5 keV and 29 keV as well as effective pixel sizes of 60 nm and 51 nm were used for the Al- Ti-based materials, respectively. Phase retrieval for holotomography was achieved from recordings at four focal-point-to-sample distances. Microstructural features as small as ( 180 nm are detected in an AlMg7Si4 alloy, a SiC particle reinforced AlCu4 alloy, a near Ti-10V-2Fe-3Al alloy, and in a TiB reinforced  Ti-6Al-4V alloy (see Fig 1).

Figure 1: Rendered volume of the minority phases in Ti64/TiB/5w: TiB needles (green) are connected to irregularly shaped  grains (other colours), forming an interpenetrating structure within the  phase.

References

[1] P. Cloetens, W. Ludwig, J, Baruchel, D. Van Dyck, J. Van Landuyt, J.P. Guigay, M. Schlenker, Appl. Phys. Lett. 75, 19, 2912-2914 (1999).

[2] R. Mokso, P. Cloetens, E. Maire, W. Ludwig, J.Y. Buffiere, Appl. Phys. Lett. 90, 14, (2007) 144104.