## Slide 1: Factors to Consider for Observing Bitumen Microstructure with Microscopy
Johannes Mirwald, Christina Niszl, Lukas Eberhardsteiner, Bernhard Hofko
Christian Doppler Laboratory for Bituminous Materials
Institute of Transportation
TU Wien

## Slide 2: Challenges while Observing Bitumen Microstructure
THE SAME BITUMEN

## Slide 3: Factors to Consider
Sample Preparation
  Homogeneity
  Heating Temperature and Time
  Impact of the Microscope
When is the best time to capturing the microstructure
  Different resting periods
  Comparing surface (brightfield) to subsurface (darkfield)

## Slide 4: Using Microscopy to Characterize Bitumen
“Nice images” versus quantification
  How can we quantify bitumen microstructure?
  Which microscopic mode is most suitable?
Differentiation between:
  Crude oil source and refinery procedure
  Ageing state
  Specification class

## Slide 5: Sample Preparation
Homogeneity and thermal history of the sample
  Stirring with a thermometer
Selection of heating temperature and time
  Temperature between 100 – 180°C, 15 secs – 10 minutes
A
B
C

## Slide 6: Microscopic Setup – Optical Microscopy
Inverse optical bright-, darkfield and fluorescence microscope
Lightsource: LED with 15 different LEDs
  500 nm
Brightfield:
  Collects all light
  Short exposure times (5 ms)
Darkfield:
  Collects all scattering light (45°)
  Longer exposure times (500 nm)
100x Nikon Plan Fluor objective
Nikon FI 3 digital camera
BF/DF/FL
Nikon
Plan Fluor
100x
365
385
405
435
365
365
470
490
500
460
365
550
580
595
525
365
660
710
770
635
Intensity
LED 365: 100%
LED Controller
Objective
Camera
Microscope
Filter Cube
Motorized Stage
Sample
LED

## Slide 7: Quantification of Microstructure
Using dark field microscopic images  Best contrast
3 x 3 samples per bitumen
Using a freeware (ImageJ Fiji©)
Image evaluation based on:
Color threshold
Particle number and size

## Slide 8: First Step: The Best Moment?
5 min
10 min
30 min
360 min
120 min
60 min

## Slide 9: Darkfield Particle Analysis

## Slide 10: Second Step: Heating Time?
15 sec
60 sec
120 sec
30 sec

## Slide 11: Impact of Heating Time and Microscope
Binder A
15 sec
30 sec
60 sec
120 sec
https://de.wikipedia.org/wiki/Deformationsschwingung (23.08.2021)
https://www.bruker.com/de/products-and-solutions/infrared-and-raman/ft-ir-routine-spectrometer/alpha-ii-compact-ft-ir-spectrometer.html (23.08.2021)
https://www.researchgate.net/figure/Schematic-representation-of-an-ATR-FTIR-system-The-infrared-beam-passes-through-the-ATR_fig1_275021699 (23.08.2021)

## Slide 12: Comparing Different Crude Oil Sources
Binder A – 70/100 pen.
Binder B – 70/100 pen.
Binder C 70/100 pen.

## Slide 13: Comparing Different Crude Oil Sources
Binder A
Binder B
Binder C
Chart: Heating time [sec]
Partikelanzahl | 294 | 299 | 274 | 292 | 256 | 300 | 258 | 258 | 265 | 306 | 313 | 282 | 255 | 275 | 273 | 265 | 268 | 250 | 246 | 282 | 288 | 229 | 275 | 254 | 266 | 261 | 278 | 237 | 239 | 239 | 226 | 234 | 244 | 238 | 226 | 194
Partikelfläche | 1908.7313 | 1784.0334 | 2062.354 | 1898.137 | 1971.7188 | 1561.21 | 1621.8605 | 1775.0969 | 1867.8943 | 1586.0098 | 1736.1885 | 1590.5816 | 1872.6745 | 1864.0545 | 1940.6593 | 1834.0604 | 2013.0821 | 2123.864 | 1733.9634 | 2092.5603 | 1795.3194 | 2304.2358 | 2022.7891 | 2040.9724 | 1993.4398 | 1939.3985 | 2122.6871 | 2211.8776 | 2320.5397 | 2057.7866 | 1943.0619 | 2298.1154 | 2322.127 | 2332.5966 | 2281.7522 | 2371.232
Chart: Heating time [sec]
Partikelanzahl | 109 | 122 | 131 | 131 | 109 | 110 | 104 | 114 | 127 | 223 | 194 | 202 | 116 | 99 | 112 | 116 | 120 | 125 | 111 | 113 | 127 | 145 | 114 | 118 | 105 | 129 | 123 | 109 | 107 | 103 | 83 | 105 | 112 | 119 | 115 | 109
Partikelfläche | 780.2936 | 714.1393 | 765.6489 | 651.2672 | 750.6881 | 582.6182 | 763.1346 | 808.2807 | 725.9134 | 324.7803 | 337.1546 | 349.4851 | 799.0086 | 853.9091 | 796.25 | 715.2845 | 711.4 | 637.32 | 750.2613 | 801.3363 | 754.6142 | 598.4483 | 743.307 | 708.9237 | 719.1143 | 716.155 | 685.3821 | 689.156 | 694.6636 | 672.6214 | 841.2771 | 759.1048 | 746.8304 | 862.0084 | 920.7652 | 755.6789
Chart: Heating time [sec]
| 30min, HP15sek 1-1 | 30min, HP15sek 1-2 | 30min, HP15sek 1-3 | 30min, HP15sek 2-1 | 30min, HP15sek 2-2 | 30min, HP15sek 2-3 | 30min, HP15sek 3-1 | 30min, HP15sek 3-2 | 30min, HP15sek 3-3 | 30min, HP30sek 1-1 | 30min, HP30sek 1-2 | 30min, HP30sek 1-3 | 30min, HP30sek 2-1 | 30min, HP30sek 2-2 | 30min, HP30sek 2-3 | 30min, HP30sek 3-1 | 30min, HP30sek 3-2 | 30min, HP30sek 3-3 | 30min, HP1min 1-1 | 30min, HP1min 1-2 | 30min, HP1min 1-3 | 30min, HP1min 2-1 | 30min, HP1min 2-2 | 30min, HP1min 2-3 | 30min, HP1min 3-1 | 30min, HP1min 3-2 | 30min, HP1min 3-3 | 30min, HP2min 1-1 | 30min, HP2min 1-2 | 30min, HP2min 1-3 | 30min, HP2min 2-1 | 30min, HP2min 2-2 | 30min, HP2min 2-3 | 30min, HP2min 3-1 | 30min, HP2min 3-2 | 30min, HP2min 3-3
Partikelanzahl | 250 | 282 | 233 | 276 | 251 | 266 | 232 | 268 | 255 | 224 | 236 | 229 | 248 | 294 | 262 | 263 | 275 | 266 | 238 | 247 | 237 | 232 | 210 | 215 | 243 | 269 | 279 | 249 | 235 | 225 | 261 | 229 | 225 | 286 | 240 | 249
Partikelfläche | 3911.54 | 3077.9716 | 3566.4936 | 3295.308 | 3301.8446 | 3594.5977 | 3565.9052 | 3408.3582 | 3436.749 | 4071.0759 | 3909.9407 | 3947.1135 | 2454.3629 | 2872.2483 | 3048.0038 | 3526.3346 | 3132.3818 | 3399.4361 | 3705.2101 | 3828.9028 | 3592.5612 | 3893.0517 | 4333.2429 | 4060.293 | 3012.2716 | 3166.8885 | 3186.8674 | 3744.8835 | 4114.5617 | 4037.0178 | 3102.7816 | 3626.4279 | 3967.7022 | 2515.6818 | 3207.7917 | 3569.4378

## Slide 14: Comparing Different Crude Oil Sources
Chart: Heating time [sec]
Partikelanzahl | 294 | 299 | 274 | 292 | 256 | 300 | 258 | 258 | 265 | 306 | 313 | 282 | 255 | 275 | 273 | 265 | 268 | 250 | 246 | 282 | 288 | 229 | 275 | 254 | 266 | 261 | 278 | 237 | 239 | 239 | 226 | 234 | 244 | 238 | 226 | 194
Partikelfläche | 1908.7313 | 1784.0334 | 2062.354 | 1898.137 | 1971.7188 | 1561.21 | 1621.8605 | 1775.0969 | 1867.8943 | 1586.0098 | 1736.1885 | 1590.5816 | 1872.6745 | 1864.0545 | 1940.6593 | 1834.0604 | 2013.0821 | 2123.864 | 1733.9634 | 2092.5603 | 1795.3194 | 2304.2358 | 2022.7891 | 2040.9724 | 1993.4398 | 1939.3985 | 2122.6871 | 2211.8776 | 2320.5397 | 2057.7866 | 1943.0619 | 2298.1154 | 2322.127 | 2332.5966 | 2281.7522 | 2371.232
Mittelwert Partikelfläche | 1827.8929 | 1827.8929 | 1827.8929 | 1827.8929 | 1827.8929 | 1827.8929 | 1827.8929 | 1827.8929 | 1827.8929 | 1840.1305 | 1840.1305 | 1840.1305 | 1840.1305 | 1840.1305 | 1840.1305 | 1840.1305 | 1840.1305 | 1840.1305 | 2005.0406 | 2005.0406 | 2005.0406 | 2005.0406 | 2005.0406 | 2005.0406 | 2005.0406 | 2005.0406 | 2005.0406 | 2237.6766 | 2237.6766 | 2237.6766 | 2237.6766 | 2237.6766 | 2237.6766 | 2237.6766 | 2237.6766 | 2237.6766
Chart: Heating time [sec]
Partikelanzahl | 109 | 122 | 131 | 131 | 109 | 110 | 104 | 114 | 127 | 223 | 194 | 202 | 116 | 99 | 112 | 116 | 120 | 125 | 111 | 113 | 127 | 145 | 114 | 118 | 105 | 129 | 123 | 109 | 107 | 103 | 83 | 105 | 112 | 119 | 115 | 109
Partikelfläche | 780.2936 | 714.1393 | 765.6489 | 651.2672 | 750.6881 | 582.6182 | 763.1346 | 808.2807 | 725.9134 | 324.7803 | 337.1546 | 349.4851 | 799.0086 | 853.9091 | 796.25 | 715.2845 | 711.4 | 637.32 | 750.2613 | 801.3363 | 754.6142 | 598.4483 | 743.307 | 708.9237 | 719.1143 | 716.155 | 685.3821 | 689.156 | 694.6636 | 672.6214 | 841.2771 | 759.1048 | 746.8304 | 862.0084 | 920.7652 | 755.6789
Mittelwert Partikelfläche | 726.8871 | 726.8871 | 726.8871 | 726.8871 | 726.8871 | 726.8871 | 726.8871 | 726.8871 | 726.8871 | 613.8436 | 613.8436 | 613.8436 | 613.8436 | 613.8436 | 613.8436 | 613.8436 | 613.8436 | 613.8436 | 719.7269 | 719.7269 | 719.7269 | 719.7269 | 719.7269 | 719.7269 | 719.7269 | 719.7269 | 719.7269 | 771.3451 | 771.3451 | 771.3451 | 771.3451 | 771.3451 | 771.3451 | 771.3451 | 771.3451 | 771.3451
Chart: Heating time [sec]
| 30min, HP15sek 1-1 | 30min, HP15sek 1-2 | 30min, HP15sek 1-3 | 30min, HP15sek 2-1 | 30min, HP15sek 2-2 | 30min, HP15sek 2-3 | 30min, HP15sek 3-1 | 30min, HP15sek 3-2 | 30min, HP15sek 3-3 | 30min, HP30sek 1-1 | 30min, HP30sek 1-2 | 30min, HP30sek 1-3 | 30min, HP30sek 2-1 | 30min, HP30sek 2-2 | 30min, HP30sek 2-3 | 30min, HP30sek 3-1 | 30min, HP30sek 3-2 | 30min, HP30sek 3-3 | 30min, HP1min 1-1 | 30min, HP1min 1-2 | 30min, HP1min 1-3 | 30min, HP1min 2-1 | 30min, HP1min 2-2 | 30min, HP1min 2-3 | 30min, HP1min 3-1 | 30min, HP1min 3-2 | 30min, HP1min 3-3 | 30min, HP2min 1-1 | 30min, HP2min 1-2 | 30min, HP2min 1-3 | 30min, HP2min 2-1 | 30min, HP2min 2-2 | 30min, HP2min 2-3 | 30min, HP2min 3-1 | 30min, HP2min 3-2 | 30min, HP2min 3-3
Partikelanzahl | 250 | 282 | 233 | 276 | 251 | 266 | 232 | 268 | 255 | 224 | 236 | 229 | 248 | 294 | 262 | 263 | 275 | 266 | 238 | 247 | 237 | 232 | 210 | 215 | 243 | 269 | 279 | 249 | 235 | 225 | 261 | 229 | 225 | 286 | 240 | 249
Partikelfläche | 3911.54 | 3077.9716 | 3566.4936 | 3295.308 | 3301.8446 | 3594.5977 | 3565.9052 | 3408.3582 | 3436.749 | 4071.0759 | 3909.9407 | 3947.1135 | 2454.3629 | 2872.2483 | 3048.0038 | 3526.3346 | 3132.3818 | 3399.4361 | 3705.2101 | 3828.9028 | 3592.5612 | 3893.0517 | 4333.2429 | 4060.293 | 3012.2716 | 3166.8885 | 3186.8674 | 3744.8835 | 4114.5617 | 4037.0178 | 3102.7816 | 3626.4279 | 3967.7022 | 2515.6818 | 3207.7917 | 3569.4378
Mittelwert Partikelfläche | 3462.0853 | 3462.0853 | 3462.0853 | 3462.0853 | 3462.0853 | 3462.0853 | 3462.0853 | 3462.0853 | 3462.0853 | 3373.4331 | 3373.4331 | 3373.4331 | 3373.4331 | 3373.4331 | 3373.4331 | 3373.4331 | 3373.4331 | 3373.4331 | 3642.1432 | 3642.1432 | 3642.1432 | 3642.1432 | 3642.1432 | 3642.1432 | 3642.1432 | 3642.1432 | 3642.1432 | 3542.9207 | 3542.9207 | 3542.9207 | 3542.9207 | 3542.9207 | 3542.9207 | 3542.9207 | 3542.9207 | 3542.9207
Binder A
Binder B
Binder C

## Slide 15: Comparing Different Ageing States
Binder A – RTFOT
Binder A – 70/100 pen.
Binder A – RTFOT+PAV

## Slide 16: Comparing Different Ageing States
Chart: Heating time [sec]
Partikelanzahl | 294 | 299 | 274 | 292 | 256 | 300 | 258 | 258 | 265 | 306 | 313 | 282 | 255 | 275 | 273 | 265 | 268 | 250 | 246 | 282 | 288 | 229 | 275 | 254 | 266 | 261 | 278 | 237 | 239 | 239 | 226 | 234 | 244 | 238 | 226 | 194
Partikelfläche | 1908.7313 | 1784.0334 | 2062.354 | 1898.137 | 1971.7188 | 1561.21 | 1621.8605 | 1775.0969 | 1867.8943 | 1586.0098 | 1736.1885 | 1590.5816 | 1872.6745 | 1864.0545 | 1940.6593 | 1834.0604 | 2013.0821 | 2123.864 | 1733.9634 | 2092.5603 | 1795.3194 | 2304.2358 | 2022.7891 | 2040.9724 | 1993.4398 | 1939.3985 | 2122.6871 | 2211.8776 | 2320.5397 | 2057.7866 | 1943.0619 | 2298.1154 | 2322.127 | 2332.5966 | 2281.7522 | 2371.232
Chart: Heating time [sec]
| 30min, HP15sek, RTFOT, 1-1 | 30min, HP15sek, RTFOT, 1-2 | 30min, HP15sek, RTFOT, 1-3 | 30min, HP15sek, RTFOT, 2-1 | 30min, HP15sek, RTFOT, 2-2 | 30min, HP15sek, RTFOT, 2-3 | 30min, HP15sek, RTFOT, 3-1 | 30min, HP15sek, RTFOT, 3-2 | 30min, HP15sek, RTFOT, 3-3 | 30min, HP30sek, RTFOT, 1-1 | 30min, HP30sek, RTFOT, 1-2 | 30min, HP30sek, RTFOT, 1-3 | 30min, HP30sek, RTFOT, 2-1 | 30min, HP30sek, RTFOT, 2-2 | 30min, HP30sek, RTFOT, 2-3 | 30min, HP30sek, RTFOT, 3-1 | 30min, HP30sek, RTFOT, 3-2 | 30min, HP30sek, RTFOT, 3-3 | 30min, HP1min, RTFOT, 1-1 | 30min, HP1min, RTFOT, 1-2 | 30min, HP1min, RTFOT, 1-3 | 30min, HP1min, RTFOT, 2-1 | 30min, HP1min, RTFOT, 2-2 | 30min, HP1min, RTFOT, 2-3 | 30min, HP1min, RTFOT, 3-1 | 30min, HP1min, RTFOT, 3-2 | 30min, HP1min, RTFOT, 3-3 | 30min, HP2min, RTFOT, 1-1 | 30min, HP2min, RTFOT, 1-2 | 30min, HP2min, RTFOT, 1-3 | 30min, HP2min, RTFOT, 2-1 | 30min, HP2min, RTFOT, 2-2 | 30min, HP2min, RTFOT, 2-3 | 30min, HP2min, RTFOT, 3-1 | 30min, HP2min, RTFOT, 3-2 | 30min, HP2min, RTFOT, 3-3
Partikelanzahl | 245 | 247 | 255 | 292 | 310 | 275 | 233 | 268 | 263 | 263 | 251 | 254 | 289 | 286 | 304 | 254 | 249 | 249 | 240 | 262 | 261 | 205 | 234 | 234 | 296 | 264 | 261 | 233 | 221 | 235 | 248 | 211 | 284 | 219 | 247 | 221
Partikelfläche | 2193.0776 | 2476.0486 | 2387.8078 | 2042.2466 | 1850.5032 | 2208.8436 | 2485.4979 | 2245.291 | 2251.8403 | 2028.0532 | 2047.745 | 2252.0472 | 1869.4394 | 1857.9895 | 1646.8421 | 1978.8858 | 2268.8916 | 2221.1727 | 2187.8375 | 2053.9466 | 2141.5785 | 3284.8 | 2789.9487 | 2966.2179 | 1923.8108 | 2298.197 | 2133.4559 | 2576.927 | 2903.991 | 2657.1745 | 1648.8831 | 2313.7062 | 2449.3873 | 2708.7991 | 2225.9676 | 2551.5928
Chart: Heating time [sec]
| 30min, HP15sek, PAV, 1-1 | 30min, HP15sek, PAV, 1-2 | 30min, HP15sek, PAV, 1-3 | 30min, HP15sek, PAV, 2-1 | 30min, HP15sek, PAV, 2-2 | 30min, HP15sek, PAV, 2-3 | 30min, HP15sek, PAV, 3-1 | 30min, HP15sek, PAV, 3-2 | 30min, HP15sek, PAV, 3-3 | 30min, HP30sek, PAV, 1-1 | 30min, HP30sek, PAV, 1-2 | 30min, HP30sek, PAV, 1-3 | 30min, HP30sek, PAV, 2-1 | 30min, HP30sek, PAV, 2-2 | 30min, HP30sek, PAV, 2-3 | 30min, HP30sek, PAV, 3-1 | 30min, HP30sek, PAV, 3-2 | 30min, HP30sek, PAV, 3-3 | 30min, HP1min, PAV, 1-1 | 30min, HP1min, PAV, 1-2 | 30min, HP1min, PAV, 1-3 | 30min, HP1min, PAV, 2-1 | 30min, HP1min, PAV, 2-2 | 30min, HP1min, PAV, 2-3 | 30min, HP1min, PAV, 3-1 | 30min, HP1min, PAV, 3-2 | 30min, HP1min, PAV, 3-3 | 30min, HP2min, PAV, 1-1 | 30min, HP2min, PAV, 1-2 | 30min, HP2min, PAV, 1-3 | 30min, HP2min, PAV, 2-1 | 30min, HP2min, PAV, 2-2 | 30min, HP2min, PAV, 2-3 | 30min, HP2min, PAV, 3-1 | 30min, HP2min, PAV, 3-2 | 30min, HP2min, PAV, 3-3
Partikelanzahl | 307 | 304 | 281 | 240 | 256 | 244 | 300 | 285 | 283 | 216 | 237 | 216 | 227 | 247 | 251 | 278 | 264 | 285 | 216 | 235 | 232 | 267 | 273 | 292 | 185 | 209 | 216 | 264 | 250 | 269 | 237 | 267 | 245 | 260 | 249 | 262
Partikelfläche | 1723.544 | 1830.0822 | 1775.7331 | 2368.3833 | 2261.4961 | 2392.2418 | 1667.28 | 1691.5263 | 1812.1378 | 2710.1667 | 2453.3376 | 2750.5602 | 2610.4141 | 2329.4939 | 2371.4462 | 1828.8381 | 1953.4811 | 1833.9789 | 2787.3657 | 2478.4043 | 2544.5129 | 1963.9625 | 1979.9414 | 1862.2705 | 3022.9351 | 3233.5311 | 3087.2917 | 2297.2803 | 2027.012 | 2156.2305 | 2439.0886 | 2153.5468 | 2596.1265 | 2033.6231 | 1911.9317 | 2187.9084
Unaged
RTFOT
RTFOT+PAV

## Slide 17: Comparing Different Ageing States
Chart: Heating time [sec]
Partikelanzahl | 294 | 299 | 274 | 292 | 256 | 300 | 258 | 258 | 265 | 306 | 313 | 282 | 255 | 275 | 273 | 265 | 268 | 250 | 246 | 282 | 288 | 229 | 275 | 254 | 266 | 261 | 278 | 237 | 239 | 239 | 226 | 234 | 244 | 238 | 226 | 194
Partikelfläche | 1908.7313 | 1784.0334 | 2062.354 | 1898.137 | 1971.7188 | 1561.21 | 1621.8605 | 1775.0969 | 1867.8943 | 1586.0098 | 1736.1885 | 1590.5816 | 1872.6745 | 1864.0545 | 1940.6593 | 1834.0604 | 2013.0821 | 2123.864 | 1733.9634 | 2092.5603 | 1795.3194 | 2304.2358 | 2022.7891 | 2040.9724 | 1993.4398 | 1939.3985 | 2122.6871 | 2211.8776 | 2320.5397 | 2057.7866 | 1943.0619 | 2298.1154 | 2322.127 | 2332.5966 | 2281.7522 | 2371.232
Chart: Heating time [sec]
| 30min, HP15sek, RTFOT, 1-1 | 30min, HP15sek, RTFOT, 1-2 | 30min, HP15sek, RTFOT, 1-3 | 30min, HP15sek, RTFOT, 2-1 | 30min, HP15sek, RTFOT, 2-2 | 30min, HP15sek, RTFOT, 2-3 | 30min, HP15sek, RTFOT, 3-1 | 30min, HP15sek, RTFOT, 3-2 | 30min, HP15sek, RTFOT, 3-3 | 30min, HP30sek, RTFOT, 1-1 | 30min, HP30sek, RTFOT, 1-2 | 30min, HP30sek, RTFOT, 1-3 | 30min, HP30sek, RTFOT, 2-1 | 30min, HP30sek, RTFOT, 2-2 | 30min, HP30sek, RTFOT, 2-3 | 30min, HP30sek, RTFOT, 3-1 | 30min, HP30sek, RTFOT, 3-2 | 30min, HP30sek, RTFOT, 3-3 | 30min, HP1min, RTFOT, 1-1 | 30min, HP1min, RTFOT, 1-2 | 30min, HP1min, RTFOT, 1-3 | 30min, HP1min, RTFOT, 2-1 | 30min, HP1min, RTFOT, 2-2 | 30min, HP1min, RTFOT, 2-3 | 30min, HP1min, RTFOT, 3-1 | 30min, HP1min, RTFOT, 3-2 | 30min, HP1min, RTFOT, 3-3 | 30min, HP2min, RTFOT, 1-1 | 30min, HP2min, RTFOT, 1-2 | 30min, HP2min, RTFOT, 1-3 | 30min, HP2min, RTFOT, 2-1 | 30min, HP2min, RTFOT, 2-2 | 30min, HP2min, RTFOT, 2-3 | 30min, HP2min, RTFOT, 3-1 | 30min, HP2min, RTFOT, 3-2 | 30min, HP2min, RTFOT, 3-3
Partikelanzahl | 245 | 247 | 255 | 292 | 310 | 275 | 233 | 268 | 263 | 263 | 251 | 254 | 289 | 286 | 304 | 254 | 249 | 249 | 240 | 262 | 261 | 205 | 234 | 234 | 296 | 264 | 261 | 233 | 221 | 235 | 248 | 211 | 284 | 219 | 247 | 221
Partikelfläche | 2193.0776 | 2476.0486 | 2387.8078 | 2042.2466 | 1850.5032 | 2208.8436 | 2485.4979 | 2245.291 | 2251.8403 | 2028.0532 | 2047.745 | 2252.0472 | 1869.4394 | 1857.9895 | 1646.8421 | 1978.8858 | 2268.8916 | 2221.1727 | 2187.8375 | 2053.9466 | 2141.5785 | 3284.8 | 2789.9487 | 2966.2179 | 1923.8108 | 2298.197 | 2133.4559 | 2576.927 | 2903.991 | 2657.1745 | 1648.8831 | 2313.7062 | 2449.3873 | 2708.7991 | 2225.9676 | 2551.5928
Chart: Heating time [sec]
| 30min, HP15sek, PAV, 1-1 | 30min, HP15sek, PAV, 1-2 | 30min, HP15sek, PAV, 1-3 | 30min, HP15sek, PAV, 2-1 | 30min, HP15sek, PAV, 2-2 | 30min, HP15sek, PAV, 2-3 | 30min, HP15sek, PAV, 3-1 | 30min, HP15sek, PAV, 3-2 | 30min, HP15sek, PAV, 3-3 | 30min, HP30sek, PAV, 1-1 | 30min, HP30sek, PAV, 1-2 | 30min, HP30sek, PAV, 1-3 | 30min, HP30sek, PAV, 2-1 | 30min, HP30sek, PAV, 2-2 | 30min, HP30sek, PAV, 2-3 | 30min, HP30sek, PAV, 3-1 | 30min, HP30sek, PAV, 3-2 | 30min, HP30sek, PAV, 3-3 | 30min, HP1min, PAV, 1-1 | 30min, HP1min, PAV, 1-2 | 30min, HP1min, PAV, 1-3 | 30min, HP1min, PAV, 2-1 | 30min, HP1min, PAV, 2-2 | 30min, HP1min, PAV, 2-3 | 30min, HP1min, PAV, 3-1 | 30min, HP1min, PAV, 3-2 | 30min, HP1min, PAV, 3-3 | 30min, HP2min, PAV, 1-1 | 30min, HP2min, PAV, 1-2 | 30min, HP2min, PAV, 1-3 | 30min, HP2min, PAV, 2-1 | 30min, HP2min, PAV, 2-2 | 30min, HP2min, PAV, 2-3 | 30min, HP2min, PAV, 3-1 | 30min, HP2min, PAV, 3-2 | 30min, HP2min, PAV, 3-3
Partikelanzahl | 307 | 304 | 281 | 240 | 256 | 244 | 300 | 285 | 283 | 216 | 237 | 216 | 227 | 247 | 251 | 278 | 264 | 285 | 216 | 235 | 232 | 267 | 273 | 292 | 185 | 209 | 216 | 264 | 250 | 269 | 237 | 267 | 245 | 260 | 249 | 262
Partikelfläche | 1723.544 | 1830.0822 | 1775.7331 | 2368.3833 | 2261.4961 | 2392.2418 | 1667.28 | 1691.5263 | 1812.1378 | 2710.1667 | 2453.3376 | 2750.5602 | 2610.4141 | 2329.4939 | 2371.4462 | 1828.8381 | 1953.4811 | 1833.9789 | 2787.3657 | 2478.4043 | 2544.5129 | 1963.9625 | 1979.9414 | 1862.2705 | 3022.9351 | 3233.5311 | 3087.2917 | 2297.2803 | 2027.012 | 2156.2305 | 2439.0886 | 2153.5468 | 2596.1265 | 2033.6231 | 1911.9317 | 2187.9084
Unaged
RTFOT
RTFOT+PAV

## Slide 18: Comparing Different Specification Classes from the Same Crude Oil Source
50/70 pen.
160/220 pen.

## Slide 19: Comparing Different Specification Classes from the Same Crude Oil Source
50/70 pen.
160/220 pen.

## Slide 20: Comparing Different Specification Classes from the Same Crude Oil Source
50/70 pen.
160/220 pen.

## Slide 21: Take Home Messages – What can we achieve with Microscopy so far?
Dark field microscopy can be used for particle analysis
Surface (brightfield) needs time to settle, while darkfield can be used immediately  30 minutes recommended
Strict preparation routing
  Heavily depends on sample preparation  Thermal History!!!
  Small quantities age very rapid!
Different crude oil sources/refinery procedures can be distinguished
Different ageing states from the same bitumen are difficult
Different specification classes follow a small trend that can be distinguished